ACTA MECHANICA SINICA, Vol.20, No.2, April 2004 	ISSN 0567-7718

The Chinese Society of Theoretical and Applied Mechanics

Chinese Journal of Mechanics Press, Beijing, China

Allerton Press, INC., New York, U.S.A.

DESIGN AND FABRICATION OF A MICRO THERMAL ACTUATOR FOR 
CELLULAR GRASPING*

CHAN Ho-Yin (Ni.~) 1 LI Wen J. (~2~)1,2,,

1 (Centre for Micro and Nano Systems, The Chinese University of Hong Kong, 
Shatin, N.t., Hong Kong SAR, China) 
2(Shenyang Institute of Automation, Chinese Academy of Sciences, Shenyang 110016, China)

ABSTRACT: The development of a novel polymer-based micro robotic gripper that can be actuated in a fluidic medium is presented in this paper. Our current work is to explore new materials and designs for thermal actuators to achieve micromanipulation of live biological cells. We used parylene C to encapsulate a metal heater, resulting in effectively a tri-layered thermal actuator. Parylene C is a bio-compatible dielectric polymer that can serve as a barrier to various gases and chemicals. Therefore, it is suitable to serve as a thermM/electrical/chemicM isolation material for protecting the metal heater from exposing to an aqueous environment. We have demonstrated parylene actuators (2 mm • 100 #m • 0.5 #m) to operate in an aqueous environment using 10 to 80 mW input power. The temperature of these actuators at full deflection was estimated to be ~ 60~ which is much lower than the typical requirement of > 100~ to actuate other conventional MEMS actuators. Danio rerio follicles in fluidic medium were captured successfully using these actuators. Moreover, these actuators were found to be responsive to moderate rise in environmentM temperature, and hence, we could vary the fluidic medium temperature to actuate trimorphs on a chip without any input of electrical energy, i.e., raising the fluidic temperature from 23~ to 60~ could actuate the trimorphs to grasp follicles of

I mm size in diameter. At 60~ the embryos inside the follicles were observed to be alive, i.e., they were still moving in the biological fluid isolated by the follicle membrane. The smallest follicles grasped were ~500/zm in diameter using 800 #mx 130 #m • 0.6 #m actuators. The fabrication process, modeling, and optimization of the trimorph actuators are presented. Based on the successful operation of these polymer-based actuators, we are currently developing multifinger thermal microgrippers for cellular grasping and manipulation, which can potentially be hybridly integrated with circuits for computer control.

KEY WORDS: thermal actuator, microgripper, cell manipulation, underwater microactuator

1 INTRODUCTION 	at once. In addition, the pipette cannot be used to rotate individual cells, a function which is highly de-

Microrobotics consists of a variety of research ar- sirable during a micro injection process. To address eas including microassembly [1] , microhandling [2], mi- these problems, we are currently developing a system cro mobile robots and etc. Some of the potential ap- that can manipulate and isolate ceils controllably, and plications of microrobotics with growing interest are that can potentially be used to conduct localized cell cell manipulation, cell isolation, and micro injection probing and measurements.

in the biomedical field. For example, biologists usu-

ally use pipettes for cell isolation prior to carrying Most of the existing MEMS actuators are limited

out micro injection. However, the functionality of this 	to specific or narrow applications due to their limited

method is limited by the size of the cells, i.e., the cells 	displacement, force output, and necessary working en-

cannot be too small compared to the pipette; other- 	vironment. As described by S. Shoji [3] , each micro

wise, a bundle of cells could be drawn into the pipette 	actuation principle, including electrostatic, piezoelec-

Received 6 August 2003

* The project supported by the Hong Kong Research Grants Council (CUHK4215/01) 
t E-maih weu@acae.cuhk.edu.hk

Vol.20, No.2 Chan HY & Li W J: A Micro

tric, electromagnetic and thermal, has their own ad- vantages and disadvantages. For example, the prob- lem encountered in electrostatic and piezoelectric is limited deflection. Magnetic actuators currently still need off-chip magnetic source to actuate them effec- tively. Thermal actuators, however, can produce large force and deflection but they require large power and may affect the temperature of the surrounding en-vironment. For the purpose of micromanipulation,

more specifically for cell manipulation, actuators are 
required to operate in biological fluid environment. 
Electrostatic actuation is inefficient in ion-rich fluid 
and the deflection is small [4] . Therefore, thermal actu-
ators were considered by some researchers to operate 
in solution-based environments. Generally speaking, 
thermal actuator consisting of two layers, in which one 
of the layers would be a heater, is called a "bimorph".

For thermal actuators to operate in for aqueous 
environments, heat convection to a solution medium 
can be as significant as conduction to the substrate. 
Consequently, micro actuation in an aqueous medium

requires much higher input power than actuation in air. Lin et al. [4] have demonstrated a 2-layer ther- mal/electrostatic actuator (200 pm x 45 #m • 1.1 pm with polyimide/Au layers). This thermal actuator can operate in air with 7V at 4mA. However, for actuation in liquid, it requires voltage as high as 100V and causes overheat of the actuator. Ataka et al. [5] also fabricated a thermal bimorph actuator (500 pm • 100 #m x 6 #m with polyimide/Au layers).

Thermal Actuator for Cellular Grasping

The temperature of the actuator rose up to 260~ for

actuation, which will definitely kill cells.

Owing to the disadvantages of silicon-and

metal-based thermal actuators to operate in aqueous

environments, new materials and designs for thermal

actuators must be explored to achieve micromanipu-

lation of live biological cells. In this paper, parylene

C is chosen to encapsulate a middle metal heater, re-

sulting in a tri-layered thermal actuator. Parylene C,

which is a polymer, has excellent mechanical and elec-

trical proprieties. Comparison between the properties

of parylene C and common used materials in MEMS

are shown in Table i. It has a large coefficient of

thermal expansion (CTE) and a high dielectric con-

stant. It can withstand temperatures up to ~ 180~

and is extremely conforma116]. It is bio-compatible

and can serve as a barrier to oxygen, moisture, chemi-

cals, solvents, and carbon dioxide. Therefore, we have

chosen it to protect the metal from exposing to fluid

while the actuator is working in an aqueous environ-

ment. Moreover, as the metal heater is covered by

parylene, heat can be trapped and thus heat loss to

the surrounding can be reduced. Also, it can protect

the metal layer from reacting with the fluid. Pary-

lene C has been used to create microfluidic devices

such as microchannel [7] and micro check valve is] by

other researchers. Here, we explore the advantage of

parylene to potentially develop a polymer-based mi-

cro thermal gripper for micromanipulation in aqueous

environment to capture cells.

Table 1 Comparison on physical properties of various thin film materials

Platinum PolySi SiO2 Parylene coefficient of thermal expansion (CTE)/K -1 9 x 10 -6 2.5 • 10 -6 12 x 10 -6 3.5 • 10 -5

density/(kg.m -3) 
Young's modulus/GPa 
thermal conductivity/(W.m-l.K -1)

2 MODELING

2.1 Design of the Dimension of Actuator

The motion of this polymer-based thermal ac-tuator can be estimated by a three-layer cantilever beam model. In our current design, the middle layer is platinum and the top and bottom layers are parylene. When current passes through the platinum, the entire structure will be heated up. Due to the difference in coefficient of thermal expansion (CTE) between plat- inum and parylene, each layer would expand differ- ently and lead to the curling up of the beam. By considering the interaction of forces and moments be- tween the layers, the bending radius of curvature r due to temperature change AT can be calculated by Eqs.(1)~(5).

| 2 145 | 2 300 | 2 300 | 1 289 |
| --- | --- | --- | --- |
| 146.9 | 170 | 83 | 3.2 |
| 69.23 | 28 | 1.38 | 0.082 |

r= (1-~AD-1C)/-AD-1BAT

1

=g(A, B, C, D). AT (1) where

A-~ tl+~-tl§ (2)

Vol.20, No.2 Chan HY & Li W J: A Micro Thermal Actuator for Cellular Grasping

interface. In: Micromechatronics and Human Science, 2001. 211~217

2 Thompson JA, Fearing RS. Automating microassem- bly with ortho-tweezers and force sensing. Intelligent Robots and Systems, 2001, 3:1327~1334

3 Shoji S, Esashi M. Microflow devices and systems.

Journal of Micromechanics and Microengineering,

1994, 4:157~171

4 Lin G, Kim C J, Konishi S, et al. Design, fabrica-tion and testing of a C-shape actuator. In: Tech Dig, Transducers '95, Stockholm, Sweden, 1995. 416~-,419

5 Ataka M, Omodaka A~ Takeshima N, et al. Fabrica- tion and operation of polyimide bimorph actuators for a ciliary motion system. Journal of Microelectrome- chanical Systems, 1993, 2(4): 146~150

6 Harder TA, Yao T J, He Q, et al. Residual stress in thin-film parylene-C. In: Proceeding of IEEE Interna- tional Conference on Micro Electro Mechanical Sys- tems (MEMS '02), Las Vegas, USA, 2002. 435~438

7 Walsh K, Norville J, Tai YC. Photoresist as a sacrifi- cial layer by dissolution in acetone. In: Proceeding of IEEE International Conference on Micro Electro Me- chanical Systems (MEMS '01), 2001. 114~117

8 Qi WX, et al. A parylene micro check valve. In: IEEE International Conference on Micro Electro Mechani- cal Systems (MEMS '99), Piseataway, N J, USA, 1999. 177~182

9 Incropera FP, DeWitt DP. Fundamentals of Heat and Mass Transfer, Wiley, 1996

10 Chan HY, Li WJ. A polymer-based micro thermal actuator for micromanipulations in aqueous environ- ment. International Journal of Non-linear Sciences and Numerical Simulation, 2002, 3(3-4): 775~778