(

Dielectrophoretic Batch Fabrication of Bundled Carbon Nanotube Thermal Sensors

Carmen K. M. Fung, Student Member, IEEE, Victor T. S. Wong, Student Member, IEEE, Rosa H. M. Chan, Student Member, IEEE and Wen J. Li, Member, IEEE, Member, ASME

Abstract—We present a feasible technology for batch assembly of carbon nanotube (CNT) devices by utilizing AC electrophoretic technique to manipulate multi-walled carbon nanotube (MWNT) bundles on a Si/SiO2 substrate. Based on this technique, CNTs were successfully and repeatably manipulated between micro-fabricated electrodes. By using this parallel assembly process, we have investigated the possibility of batch fabricating functional CNT devices when an AC electrical field is applied to an array of microelectrodes which are electrically connected together. Preliminary experimental results showed that over 70% of CNT functional devices can be assembled successfully using our technique, which is considered to be a good yield for nanodevices manufacturing. Besides, the devices were demonstrated to potentially serve as novel thermal sensors with low power consumption (~ (W) with electronic circuit response of about 100 kHz in constant current mode operation.  In this paper, we will present the fabrication process of this feasible batch manufacturable method for functional CNT based thermal sensors, which will dramatically reduce production costs and production time of nano sensing devices and potentially enable fully automated assembly of CNT based devices. Experimental results from the thermal sensors fabricated by this batch process will also be discussed.

Index Terms— AC electrophoretic manipulation, carbon nanotube, CNT sensors, nano manufacturing, nano batch fabrication.

# INTRODUCTION

Carbon nanotubes (CNTs), since discovered in 1991 by Sumio Iijima [1], have been extensively studied for their electrical (e.g., see [2]) and mechanical properties (e.g., see [3]). Owing to their minute dimensions, and good mechanical and electrical properties, different groups started to utilize CNTs as nano sensors or actuators for different applications in nanoelectronic or nano-electro-mechanical systems (NEMS). For example, CNT has been found to be an excellent 1-D quantum wire [2], nano-transistor [4], molecular random access memory [5] for nanoelectronic applications and more recently the nano-motor with CNT as a rotational shaft for NEMS application [6].

In order to build practical CNT based devices, fast and batch techniques to manipulate the CNTs have to be developed.  However, CNTs tend to cling together in nature due to the presence of strong surface charges on their surfaces. The difficulty of isolating a single CNT from an intertwined bundle without tremendous effort in the sense of batch fabrication has led to a clear boundary between the two approaches of the usage of CNTs: either to treat each CNT as an individual building element, or to treat CNT bundles (or array) as a whole building block.

To fabricate a nanodevice with CNTs as individual building elements, the basic requirements include the isolation, manipulation, transport, fixture and connection, etc., of a single CNT. Typical manipulation technique is by atomic force microscopy [7] and a variety of mechanical and electronic nanodevices have been fabricated by using AFM based assembly method (e.g., see [8]). However, even though the AFM based technique has very high positioning accuracy, this pick-and-place technique is time consuming, and few efforts have been reported to tackle the fundamental problem of the inefficiency caused by AFM operations when the process turns into batch production. Among which, Kim et al., have reported a method to align CNTs side by side by means of condensation of nanowire solution [9][10]. On the other hand, bypassing the complex AFM operations completely, some of the nanodevice researchers have shifted to focus on treating CNT/nanowire bundles as an individual functional (e.g., sensing) element. By means of chemical vapor deposition (CVD), in combination with lithography techniques [11] or laser trimming [12], “vertically” aligned CNT/nanowires can be grown and patterned on specific sites in batch mode. The nanodevices developed based on this approach generally treat a bundle of aligned CNT/nanowires as one functional (i.e., sensing, emitting, etc.,) element. By patterning an array of “functional bundle”, a functional array is formed.  On the other hand, electric-field assist assembly is another feasible technology in batch fabrication of CNT/nanowires devices.  K. Yamamoto et al., have pioneered the work in electric-field assist manipulation of CNT bundles [13][14]. The usage of electric-field assist assembly has also been reported for batch assembly of nanowires as well [15].  Recently, Nagahara et al., have demonstrated the manipulation of CNT strands by AC bias voltage to form functional nano-resistive device between a pair of nano-electrodes [16].  Based on the technique of electric-field assist assembly (i.e., AC electrophoresis), we have successfully manipulated bundled CNTs to connect between an array of microelectrodes and we have also preliminarily proven that CNT device is capable of very low power thermal sensing and can be fabricated in a fast and efficient manner.

This paper reports the AC electrophoretic technique to form bundled MWNT resistive elements between gold (Au) microelectrodes which were fabricated by a standard microlithographic technique. In addition, the experimental results showing the validity of batch assembling of arrays of CNT sensors by AC electrophoresis will be presented. Besides, the electrical performance of the assembled CNT devices such as I-V characteristics, frequency response and temperature coefficient of resistance (TCR) will be characterized and presented in later sections.

# AC Electrophoretic Manipulation Of Carbon Nanotube

## Theoretical Background and Modeling

AC electrophoresis (or dielectrophoresis) is a phenomenon where neutral particles undergo mechanical motion inside a non-uniform AC electric field [17] (see Fig. 1).

In our CNTs manipulation experiments, CNTs were dispersed inside a liquid medium (e.g., ethanol) and therefore other forces (e.g., viscous force) besides dielectrophoretic forces are imparted on CNTs during the manipulation process.  In order to understand the physical phenomenon during the AC electrophoretic manipulation, we have conducted the following simulations with experimental verifications on the effect of CNT alignments on different microelectrode geometries.

During the CNTs manipulation, the total force acting on a MWNT is the sum of a number of independent forces [18][19]. With negligible gravitational force, the three dominate force components are the dielectrophoretic (DEP) force, viscous force and the electro thermal force. For other small particles with volumes compatible to MWNT, thermal effects can dominate, but the high polarizability of MWNT makes the DEP force large enough to produce deterministic movements.

Dielectrophoresis refers to the force exerted on a polarized particle in the non-uniform electric field [17][20]. It can be written as

(1)

where E is the electric field, m is the induced dipole moment of MWNT. Assumed that the MWNT is a long prolate spheroid with the longest axis aligned with the electric field, the induced dipole moment is

(2)

where , a and b are absolute permittivity of the medium, the half length of MWNT and the radius of MWNT,  respectively. Therefore, the complex polarization factor K is given by

(3)

where  and  are the absolute complex permittivities of MWNT [21] and the medium (ethanol) [22], respectively, and the approximated depolarization factor [20] . Since the electric field components are in phase, the time averaged DEP force deduced from the above equations is

(4)

where  is the gradient of the square of the root-mean-square of the electric field. The gradient is affected by both the geometry of the electrodes and the applied voltage. The former factor gives the overall position of the MWNT branches between the electrodes because it determines the direction of the average DEP force. As the potential difference applied is proportional to the magnitude of electric field, a larger potential can increase the magnitude of the DEP force and offer a larger torque to align the MWNT with the electric field direction [20].

Frequency of the applied voltage also affects the magnitude of DEP force as the complex permittivity spectra of MWNT and ethanol are the functions of the frequency [21][22][23]. Because of the high conductivity of the assumed purified MWNT ((2.22 x 104S/m) [21] and the small depolarization factor resulted from its long dipole (8.3434 x 10-5), the real part of the complex polarization factor is positive as shown in Fig. 2. Although the actual complex polarization factor varies, which is because the absolute permittivity and the orientation of each MWNT varies [21], Re(K) remains positive. When substituting different permittivity values at 1MHz, the DEP force is maximum when the longest axis is parallel to the electric field (Re(K)(3995.2).  By substituting with in (3), the minimum DEP force can be calculated when it is perpendicular to the field (Re(K)(0.6667). The corresponding positive dielectrophoretic force draws the MWNT to the electric field maxima.

Another factor affecting the magnitude of the force is the volume of the MWNT as shown in (4). In the MWNT manipulation experiment, MWNT with axial length and diameter about 1-10 μm and 10-30 nm, respectively, was used, and therefore, a = 2.5 μm and b = 10 nm are taken as the averages in the simulation.

A few microelectrodes with different geometries were fabricated and the CNT connections across the microelectrodes by AC electrophoresis are shown in Fig. 3(a) to Fig. 3(c).  Detailed experimental procedures in forming CNT bundles across microelectrodes will be presented in next section.  However, in order to visualize the electric field distribution generated by different microelectrode geometries, simulations were conducted and are described in the following part.

The approximate order-of-magnitude of the potential was investigated by using Green’s theorem [24], where the square of the root-mean-square magnitude of the field is calculated using MatLab. Since the magnitude of the electric field decreases with height away from the substrate, the positive DEP draws the MWNT downwards to the edges of the electrodes. The force fields in Fig. 4 and Fig. 5 are estimated by (4), assuming the longest axes of MWNT is parallel to instantaneous electric field.

Downward forces are shown by the contours in Fig. 4(a) and Fig. 4(b) between the electrodes and close to the electrode surfaces. The DEP forces are significantly large to draw the MWNT downwards and to overcome the upward movement from electro thermal effect [19].

The time averaged alignment torque acting on the MWNT causes them to direct as the electric field vectors. As the electric field intensity is higher at the closest corners between electrodes, the MWNT are drawn to their edge.  When a MWNT touches one of the electrodes, it shares the same potential as the electrode and thus the electric field intensity is modified to be higher at its free end. Therefore, the nanotubes near it tend to stick to it. When the nanotube bridges the adjacent voltages, the branching structures between electrodes are formed [13] as in Fig. 3.  Details of experimental procedures for the AC electrophoretic manipulation of MWNT will be presented in the next section.

## Experimental Details and Results

Based on the physical phenomenon of AC electrophoresis, we have successfully manipulated the bundled CNTs on fabricated microelectrodes. The experimental process flow for the CNTs manipulation can be divided into three parts: fabrication of microelectrodes, sample preparation and experimental testing (see Fig. 6).

The Au microelectrodes were fabricated on glass or Si/SiO2 substrates by a standard microfabrication technique, which was described previously in [25].  Prior to the MWNT manipulation, bundled MWNTs were prepared by a sonication treatment. The bundled MWNTs used in the experiments were ordered commercially from [26] which were prepared by chemical vapour deposition.  The axial dimension and the diameter of the MWNTs was 1 – 10 µm and 10 – 30 nm, respectively. In order to form stable colloidal suspension of MWNTs and minimize the degree of aggregation, 50 mg of the sample was ultrasonically dispersed in 500 mL ethanol solution and the resulting solution was diluted to 0.01 mg/mL for later usage.

During the CNTs manipulation, a substrate with fabricated Au microelectrodes was placed on the vacuum pump based stage of a micromanipulator station, which allowed the probing of microelectrodes by microprobes. Au microelectrodes were then excited by an AC voltage source with typically of 16 V peak-to-peak with frequency of 1 MHz. Approximately 10µL of the MWNTs/ethanol solution was transferred to the substrate by a 6 mL gas syringe. The ethanol was evaporated away leaving the MWNTs to reside between the gaps of the microelectrodes. We have observed from the experimental results that bundled MWNTs was attracted towards the Au microelectrodes under non-uniform electric field (see Fig. 7) and connected across the microelectrodes.  A representative scanning electron microscopic (SEM) image showing the bridging of MWNTs across the Au microelectrodes is shown in Fig. 8.

The formation of MWNTs linkages can be further confirmed by testing the connectivity between the pair of microelectrodes. For instance, room temperature resistances between the microelectrodes were measured and the two probe room temperature resistances of the samples typically range from several kΩ to several hundred kΩ, which suggested the connection had been formed between the two microelectrodes. Since the conductivity of CNTs depend on their lattice geometries during their growth process, the conductivities of individual CNTs cannot be well controlled, which results in the variation of conductivities in individual CNTs.  During the AC electrophoresis process to form MWNT bundles across microelectrodes, the MWNTs were randomly connected between microelectrodes.  Therefore, it is logical that different MWNT samples exhibited different conductivities.

As mentioned in the pervious section, AC electrophoretic manipulation is different from those traditional pick-and-place manipulations (e.g., AFM manipulation) which can only assemble CNT devices one at a time. Instead, AC electrophoretic manipulation is a parallel assembly process where batch assembly of CNT devices is theoretically possible when the electrical potential is applied to an array of microelectrodes which are connected electrically together. To prove the validity of batch assembling by AC electrophoresis, we have implemented the experimental procedures mentioned and extended to an array of Au microelectrodes which are electrically connected together on a substrate (see Fig. 9). By using the same experimental parameters presented before, we have successfully manipulated the CNT bundles on most of the Au microelectrodes by AC electrophoresis in a single-run fashion. The connections of bundled CNTs for different pairs of microelectrodes on a substrate after addition of one drop of MWNTs/ethanol solution (~ 10µL) were shown in Fig. 10. In order to confirm the linkage of bundled CNTs across two microelectrodes, the room temperature resistance corresponding to each pair of microelectrodes was measured. The CNT connection process was deemed successful between 2 microelectrodes when the room temperature resistance measured became several kΩ to several hundred kΩ. Several chips were then checked using a scanning electron microscope (SEM) to validate the CNT connections between the electrodes.

To validate the consistency of the batch assembly of CNT devices, repeated experiments for AC electrophoretic batch manipulation of CNTs between the arrays of Au microelectrodes were performed and plots of statistical data for different experiments were generated (see Fig. 11), which shows the maximum, minimum, average and standard deviation (S. D.) among the measured resistances on each sample. From the experimental results, we have observed that the range of the room temperature resistances is from several kΩ to several hundred kΩ as stated earlier. Besides, we have experimentally found that the success rate for different sensor chips are consistent with overall success rate, which is equal or greater than 70%.  The success rate is defined as the ratio of the number of successful CNTs-connected microelectrodes to the total number of microelectrodes on a substrate.  Since the volume of each drop of the CNTs/ethanol solution in the experiment is not consistent, the yield of the batch assembly of the bundled CNTs cannot be 100% based on our current rudimentary technique. However, the batch AC electrophoretic manipulation of bundled CNTs is efficient and reliable based on our experimental validation, and the yield can be further improved by using a more precise injection system.

# Carbon Nanotube As Sensing Elements For Thermal Sensing

With the ability to batch manipulate the bundled CNTs to form resistive elements on patterned substrates, we have investigated the possibility to utilize the bundled CNTs as sensing elements for thermal sensing. In the following sections, we will present our preliminary electrical characterizations on thermal sensitivity, frequency response and I-V response of the sensors.

## Thermal Sensitivity

In order to investigate the temperature dependence of the bundled MWNT sensors, several fabricated sensor chips were packaged on a PCB for data acquisition and were put inside an oven (L-C Oven Lab-Line® Instrument Inc., USA).  The oven temperature was monitored by a Fluke type-K thermocouple attached on the surface of the PCB circuit board. Then, the resistance change of the MWNT sensors were measured against the temperature inside the oven. The temperature-resistance relationship for the MWNT sensors was measured and a representative data set is shown in Fig. 12 for several cycles of measurements after a few thermal annealing cycles.  From the experiments, it was found that a few thermal annealing cycles (from 25oC to 80oC for ~ 5 cycles) were necessary before the measured temperature coefficient of resistances (TCRs) of the sensor can be stabilized, i.e., considerably room temperature resistances drift were observed in repeated measurements during the thermal annealing cycles.  The statistical data of the room temperature drift of a typical CNT sensor for each cycle of measurement was measured and plotted in Fig. 13. It was found that the magnitude of the change in resistance during the annealing is ~ 40% after ~ 5 cycles. The resistance would stabilize afterwards. One possible reason to account for this phenomenon is that during the thermal cycling processes, some CNTs with weak adhesion with the Au microelectrodes may detach from them due to mismatch in temperature coefficient of expansion, causing the drift of the room temperature resistance after each thermal cycling. Therefore, our current work is to use polymer thin films to protect the CNTs and provide a better fixture of CNTs with the microelectrodes.

The temperature coefficient of resistance (TCR) of the bundled MWNT sensors was measured to determine their thermal sensitivity. From the experimental results, the bundled MWNTs were sensitive to the change of temperature and their resistance dropped with increasing temperature. The negative TCR of the MWNTs has been reported previously in [27], though the measurements were based on individual MWNTs. The temperature-resistance dependency of bundled MWNTs implied their thermal sensing capability. Based on experimental results, the TCR for a MWNT sensor was obtained by measuring the resistance change of the bundled MWNTs with the corresponding temperature and calculated based on (5):

(5)

where  is the resistance at room temperature , and  is the temperature coefficient of resistance. The range of the TCR for the MWNT sensors was found to be from -0.1 to -0.2.

## Power Consumption

Electrical properties of individual CNTs have been studied by many research groups [27][28] in the past few years. In this work, we have determined the I-V characteristics of the bundled MWNTs after hybridly integrating the bundled MWNTs into a constant current configuration. Similar to those of individual CNTs reported by other researchers, the bundled MWNTs also showed µW power characteristics (see Fig. 14), though bundled MWNTs can be regarded as a complex network of individual CNTs. From the results of experiments conducted on the MWNT sensors, the current required to induce self heating of the MWNT devices was in (A range at several volts, which suggests that bundled CNTs could be used as resistive element for ultra low power consumption devices. Typically, the two-probe room temperature resistance of the bundled MWNTs ranged from several kΩ to several hundred kΩ as reported previously, and we conjecture that these variations were mainly contributed by the random connections between MWNT bundles during the AC electrophoresis process. However, there are other possible factors as it is generally recognized that the CNT resistance among many reported experiments varied (e.g., see [29] and [30]). It was reported in [29] that several factors such as quality of the nanotubes and the electrical contacts may account for the variations of the measured resistance across CNTs. The existence of metal-nanotube contact resistance was explained theoretically in [30], i.e., in an idealized model, conduction between the CNT and metal may be forbidden by the Block symmetry of the electrodes. On the other hand, it was studied experimentally that contact resistance in the order of hundreds of k( or M( was measured when positioning a single CNT on a metal electrode [31] or depositing metal electrodes across a selected signal CNT [32]. Besides, it was indicated in [33] that contact resistance exists between the nanotube bundles and the metal electrodes due to observed discrepancy of three orders of magnitude when different methods were used to measure the resistance. Therefore, the contact resistance should have an influence on the variation of resistance. The magnitude of contact resistance of our sensors has to be further investigated in the future. Nevertheless, several groups have reported that the contact resistance can be decreased by orders of magnitudes by post-treatments such as local electron beam exposure [29], rapid thermal annealing process [34], electroplated Au over the contacted electrodes [35], and focused ion beam to deposit metal on CNT, which showed that the contact resistances were decreased below 100( or in the range of a few tens of (s [31]. Hence, future work for our group will involve applying one of these techniques to reduce the contact resistance of the CNT sensors.

Despite the random variations in room temperature resistance of different MWNT bundles, it was found that all of the samples have similar I-V characteristics. In comparison, the operation power of conventional MEMS polysilicon sensors is in the order of mW [36]. In other words, the power consumption of CNT based sensors is three orders of magnitude lower than that of MEMS polysilicon based sensors.

## Frequency Response of the Electronic Circuit with bundled MWNT as Feedback Resistor

Frequency response of a sensor measures its efficiency to pick up time-dependent input changes from the surrounding environment.  In order to pick up time dependent fluctuations of the sensing environment, sensors with fast frequency response are highly desired. For turbulent boundary layer research in the field of aerodynamics, shear stress sensors with fine resolution (< 100 µm), fast frequency response (> 5 kHz) and high sensitivity are highly sought [37].

A typical bundled MWNT sensing element was connected in constant current mode configuration in the frequency response experiment (see Fig. 15). To test the frequency response of the driving circuitry with bundled MWNT as feedback resistor, input square wave of 2 V peak-to-peak at 10 kHz was fed into the negative input terminal of the circuit shown in Fig. 15 and the output response was determined (see Fig. 16). From our experimental measurements, the electronic circuit with bundled MWNT as feedback resistor exhibited very fast frequency response to the input electronic signal. Using the approximation between the time constant and cutoff frequency [36],

(6)

whereis the cutoff frequency, is the time constant of the response, the estimated cutoff frequency of the system was about 177 kHz. As a comparison, typical frequency response of the constant current mode circuitry with MEMS polysilicon sensors as feedback resistors without frequency compensation is around several hundred Hz to several kHz [38].

# Conclusion

A technique to batch fabricate nano-sensors with CNTs based on dielectrophoretic manipulation was presented. We have proven that the success rate for batch assembling bundled CNTs on arrays of microelectrodes is equal or greater than 70%, which demonstrated that dielectrophoretic manipulation is a feasibility technology to batch assemble CNT functional devices. We have also proven that AC electric field can direct MWNTs to specific areas of electro-patterned substrates. With specially designed microelectrodes, bundled MWNTs can be aligned into different directions according to the electric field generation. The simulation results for the electric field distribution for different designs of microelectrode geometries were also presented. With the ability to manipulate the bundled MWNTs on microfabricated electrodes, bundled MWNTs were investigated as a sensing element for micro thermal sensing applications. We have successfully integrated the CNT sensor into constant current mode configuration for dynamic characterizations such as frequency response, and also for I-V and TCR measurements. Due to the ultra low power consumption (in the range of µW) and fast frequency response (~ 100 kHz) of the electronic circuit with bundled MWNT as feedback resistors, CNT based sensors were shown to be promising in thermal sensing applications.

Acknowledgment

The authors would like to sincerely thank Dr. W.Y. Cheung of the Department of Electronic Engineering of CUHK and Mr. King W. C. Lai and Mr. Gordon M. H. Chan of the Centre for Micro and Nano Systems of CUHK for their help and discussion on this project.

References

- S. Iijima, “Helical microtubules of graphitic carbon”, Nature, vol. 354, pp. 56 – 58, 1991.

- S. Frank, P. Poncharal, Z.L. Wang, and W.A. de Heer, “Carbon nanotube quantum resistors”, Science, vol. 280, pp. 1744 – 1746, 1998.

- E.W. Wong, P.E. Sheehan, and C.M. Lieber, “Nanobeam mechanics: elasticity, strength, and toughness of nanorods and nanotubes”, Science, vol. 277, pp.1971 – 1975, 1997.

- S.J. Tans, A.R.M. Verschueren, and C. Dekker, “Room-temperature transistor based on a single carbon nanotube”, Nature, vol. 393, pp. 49 – 52, 1998.

- T. Rueckes, K. Kim, E. Joselevich, G.Y. Tseng, C. Cheung, and C.M. Lieber, “Carbon nanotube based nonvolatile random access memory for molecular computer”, Science, vol. 289, pp. 94 – 97, 2000.

- A.M. Fennimore, T.D. Yuzvinsky, W.Q. Han, M.S. Fuhrer, J. Cumings, and A. Zettl, “Rotational Actuators Based on Carbon Nanotubes”, Nature, vol. 424, pp. 408 – 410, 2003.

- T. Shiokawa, K. Tsukagoshi, K. Ishibashi, and Y. Aoyagi, “Nanostructure construction in single-walled carbon nanotubes by AFM manipulation”, in Proc. Microprocesses and Nanotech. Conf., Japan, pp. 164-165, 2001.

- P.A. Willams, S.J. Papadakis, and M.R. Falvo, “Controlled placement of an individual carbon nanotube onto a microelectromechanical structure”, Appl. Phys. Lett., vol. 80, no. 14, pp. 2574 –  2576, 2002.

- F. Kim, S. Kwan, J. Akana, and P. Yang, “Langmuir-blodgett nanorod assembly”, J. of Am. Chem. Soc., vol. 123, no. 18,  pp. 4360 – 4361, 2001.

- D. Appell, “Wired for success”, Nature, vol. 419, pp. 553 – 555, 2002.

- B.Q. Wei, R. Vajtai, Y. Jung, J. Ward, R. Zhang, and G. Ramanath, P.M. Ajayan, “Organized assembly of carbon nanotubes”, Nature, vol. 416, pp. 495 – 496, 2002.

- F.C. Cheong, K.Y. Lim, C.H. Sow, J. Lin, and C.K. Ong, “Large area patterned arrays of aligned carbon nanotube via laser trimming”, Nanotechnology, vol .14, pp. 433 – 437, 2003.

- K. Yamamoto, S. Akita, and Y. Nakayama, “Orientation of carbon nanotubes using electrophoresis”, Japanese J. Appl. Phys., vol .35, pp. L917 – 918, 1996.

- K. Yamamoto, S. Akita, and Y. Nakayama, “Orientation and purification of carbon nanotubes using AC electrophoresis”, J. Phys. D: Appl. Phys., vol. 31, pp. L34 – L36, 1998.

- P.A. Smith, C.D. Nordquist, T.N. Jackson, T.S. Mayer, B.R. Martin, J. Mbindyo, and T.E. Mallouk, “Electric-field assisted assembly and alignment of metallic nanowires”, Appl. Phys. Lett., vol. 77, no. 9, pp. 1399 – 1401, 2000.

- L.A. Nagahara, I. Amlani, J. Lewenstein, and R.K. Tsui, “Directed placement of suspended carbon nanotubes for nanometer-scale assembly”, Appl. Phys. Lett., vol. 80, no. 20, pp. 3826 – 3828, 2002.

- H. A. Pohl, “Dielectrophoresis: the behaviour of neutral matter in nonuniform electric fields”, Cambridge: Cambridge University Press, 1978.

- A. Ramos, H. Morgan, N. G. Green, and A. Castellanos, “AC electrokinectics: a review of forces in microelectrode structures”, J. Phys. D: Appl. Phys., vol. 31, pp. 2338 - 2353, 1998.

- T. Heida, W. L. C. Rutten, and E. Marani, “Understanding dielectrophoretic trapping of neuronal cells: modeling electric field, electrode-liquid interface and fluid flow”, J. Phys. D: Appl. Phys., vol. 35, pp.1592 - 1602, 2002.

- T. B. Jones, “Electromechanics of particles”, Cambridge: Cambridge University Press, 1995.

- C. A. Grimes, E. C. Dickey, C. Mungle, K. G. Ong, and D. Qian, “Effect of purification of the electrical conductivity and complex permittivity of multiwall carbon nanotubes”, J. Appl. Phys., vol. 90, no. 8, pp. 4134 – 4137, 1995.

- P. Petong, R. Pottel, and U. Kaatze, “Water-ethanol mixtures at different compositions and temperatures. A dielectric relaxation study”, J. Phys. Chem. A, vol. 104, pp. 7420-7428, 2000.

- X-B. Wang, Y. Huang, R. Hoizel, J. P. H. Burt, and R. Pethig, “Theoretical and experimental investigations of the interdependence of the dielectric, dielectrophoretic and electrorotational behavior of colloidal particles”, J. Phys. D: Appl. Phys., vol. 26, pp. 312-322, 1993.

- X. Wang, X-B Wang, F. F. Becker, and P. R. C. Gascoyne, “A theoretical method of electrical field analysis for dielectrophoretic electrode arrays using Green’s theorem”, J. Phys. D: Appl. Phys., vol. 29, pp.1649 – 1660, 1996.

- V.T.S. Wong, and W.J. Li, “Dependence of AC electrophoresis carbon nanotube manipulation on microelectrode geometry”, Int. J. Nonlinear Sciences and Numerical Simulation., vol. 3, nos. 3-4, pp. 769-774, 2002.

- Sun Nanotech Co Ltd, Beijing, P.R. China.

- T.W. Ebbesen, H.J. Lezec, H. Hiura, J.W. Bennett, H.F. Ghaemi, and T. Thio, “Electrical conductivity of individual carbon nanotubes”, Nature, vol. 382, pp. 54 – 56, 1996.

- P.G. Collins, M.S. Arnold, and P. Avouris, “Engineering carbon nanotubes and nanotube circuits using electrical breakdown”, Science, vol. 292, pp. 706 – 709, 2001.

- A. Bachtold, M, Henny, C. Terrier, C. Strunk, and C. Schonenberger, “Contacting carbon nanotubes selectively with low-ohmic contacts for four-probe electric measurements”, Appl. Phys. Lett., vol. 73, no. 2, pp. 274 – 276, 1998.

- J. Tersoff, “Contact resistance of carbon naotubes”, Appl. Phys. Lett., vol. 74, no. 15, pp. 2122 – 2124, 1999.

- B. Q. Wei, R. Vajtai, and P. M. Ajayan, “Reliability and current carrying capacity of carbon nanotubes”, Appl. Phys. Lett., vol. 79, no. 8, pp. 1172 – 1174, 2001.

- F. Wakaya, K. Katayama, and K. Gamo, “Contact resistance of multiwall carbon nanotubes”, Microelectronic Engineering, vol. 67 – 68, pp. 853 –857, 2003.

- L. Marty, V. Bouchiat, A.M. Bonnot, M. Chaumont, T. Fournier, S. Decossas, and S. Roche, “Batch processing of nanometer-scale electrical circuitry based on in-situ grown single-walled carbon nanotubes”, Microelectronic Engineering, vol. 61 – 62, pp. 485 – 489, 2002.

- J. O. Lee, C. Park, J. J Kim, J. H. Kim, K. W. Park, and K. H. Yoo, “Formation of low-resistance ohmic contacts between carbon carbon naotube and metal electrodes by a rapid thermal annealing method”, J. Phys. D: Appl. Phys., vol. 33, pp. 1953 - 1956, 2000.

- Derek W. Austin, Alex A. Puretzky, David B. Geohegan, Phillip F. Britt, Michael A. Guillorn, and Michael L. Simpson, “The electrodeposition of metal at metal/carbon nanotube junctions”, Chem. Phys. Lett., vol. 361, pp. 525 - 529, 2002.

- C. Liu, J.B. Huang, Z. Zhu, F. Jiang, S. Tung, Y.C. Tai, and C.M. Ho, “A micromachined flow shear-stress sensor based on thermal transfer principle”, J. MEMS, vol. 8, no. 1, pp. 90 – 99, 1999.

- J.B. Huang, C. Liu, F. Jiang, S. Tung, Y.C. Tai, and C.M. Ho, “Fluidic shear stress measurement using surface-micromachined sensors”, in Proc. IEEE Region 10 Int’l Conf. Microelectronics and VLSI, Hong Kong, pp. 16 –19, 1995.

- J.B. Huang, F.K. Jiang, Y.C. Tai, and C.M. Ho, “MEMS-based thermal shear-stress sensor with self-frequency compensation”, Meas. Sci. Technol., vol. 10, no. 8, pp. 687 – 696, 1999.

Carmen Kar Man FUNG received her B.Eng. in Mechanical and Automation Engineering and M. Phil. in Automation and Computer-Aided Engineering from The Chinese University of Hong Kong (CUHK) in 2000 and 2002, respectively. She is currently pursuing her Ph.D. degree in the Department of Automation and Computer-Aided Engineering of The Chinese University of Hong Kong. Her research interest is to develop technologies for micro/nano automation and manipulation, and micro/nano sensors. Ms. Fung is a student member of IEEE. She received the Best Student Paper Award from the IS2000 in 2000, the Academic Creativity Award from the Chung Chi College, CUHK in 2000 and the Best Poster Paper Award of IEEE International Conference on Nanotechnology 2003, San Francisco, USA.

Victor Tak Sing WONG received his B.Eng. in Automation and Computer-Aided Engineering from the Chinese University of Hong Kong (CUHK), Hong Kong, in 2003. He was a student researcher in Centre for Micro and Nano Systems of CUHK from 2001 to 2003.  Currently, he is pursuing his M.Sc. in the University of California, Los Angeles (UCLA), USA.  Besides, he is working as a graduate student researcher in the Institute for Cell Mimetic Space Exploration (CMISE).  His current research interests include the development of micro/nano manipulation technologies, micro/nano fabrication technologies and micro/nano sensors and actuators. Mr. Wong is a student member of IEEE.  He received the Lucent Global Science Scholar Award in 2001, the second prize award of IEEE Region 10 Undergraduate Student Paper Contest in 2003 and the Best Poster Paper Award of IEEE International Conference on Nanotechnology 2003, San Francisco, USA.

Rosa Ho Man CHAN received her B.Eng. in Automation and Computer-Aided Engineering from The Chinese University if Hong Kong (CUHK), Hong Kong, in 2003. She is currently pursuing her M.Phil. degree in the Department of Automation and Computer-Aided Engineering. Her research interest is to develop micro/nano manipulation technologies.  Ms. Chan is a student member of IEEE and Hong Kong Institution of Engineers (HKIE).   She had studied in New York University for computer animation and visual effects in 2001, which was supported by the Hong Kong Productivity Council and Film Development Fund. Funded by a scholarship from the Association of International Exchange, Japan, she joined the University Mobility in Asia and the Pacific (UMAP) Leaders Program and worked in the Aerospace Applied Physics Laboratory of the Department of Aeronautics and Astronautics, Kyushu University in 2002. She also received the scholarship from the HKIE Manufacturing and Industrial Engineering Division in 2003.

Wen Jung LI received the B.S. and M.S. degrees in Aerospace Engineering from USC in 1987 and 1989, respectively.  His industrial experience includes The Aerospace Corporation (El Segundo, CA, USA), Silicon Microstructures Inc. (Fremont, CA, USA), and the NASA/CalTech Jet Propulsion Laboratory (Pasadena, A, USA). He obtained his Ph.D. degree from UCLA in 1997 specializing in MEMS.  He received the Aerospace Corporate Fellowship, Silicon Microstructures Inc. Employee Award, and a NASA technical innovation award for his contributions to those organizations.  Prof. Li joined the Department of Automation and Computer-Aided Engineering of The Chinese University of Hong Kong (CUHK) in 1997. In the past 6.5 years he has published more than 130 papers in international journals and conference proceedings on MEMS and nanotechnology related work. Dr. Li is currently the Guest Editor for the Focused Section on Micro and Nano Manipulations of the IEEE/ASME Transactions of Mechatronics, serving as the Director of the Centre for Micro and Nano Systems at CUHK, and also a member of the Technical Committee on Nanorobotics and Nanomanufacturing of the IEEE Nanotechnology Council. He is also a Distinguished Overseas Scholar of the Chinese Academy of Sciences. His research interest is to develop MEMS devices for micro/nano sensing and manipulation.

# Footnotes

Manuscript received August 13, 2003. This work was funded by the the Hong Kong Research Grants Council (CUHK4206/00E and 4381/02E), and the Chinese Academy of Sciences’ Distinguished Overseas Scholar Grant. This paper is based on the work presented at IEEE Nano, San Francisco, USA, August 2003.

Carmen K.M. Fung, Rosa H.M. Chan and Wen J. Li are with the Centre for Micro and Nano Systems, The Chinese University of Hong Kong, Shatin, New Territories, Hong Kong SAR.  Victor T.S. Wong was with the Centre for Micro and Nano Systems, The Chinese University of Hong Kong. He is now with the Department of Mechanical and Aerospace Engineering, The University of California, Los Angeles, CA90095, USA (email: assayer@ieee.org).  Wen J. Li is also an affiliated professor at the Shenyang Institute of Automation, Shenyang, China (email: wen@acae.cuhk.edu.hk).

# Text boxes

Fig. 8. Scanning electron microscopic (SEM) image showing the formation of MWNTs between a pair of parallel Au microelectrodes.

Fig. 1.  Magnetization as a function of applied field. Note that “Fig.” is abbreviated. There is a period after the figure number, followed by two spaces. It is good practice to explain the significance of the figure in the caption.

Fig. 6. Experimental setup for CNT manipulation by using AC electrophoresis.

Fig. 3. Experimental alignments of MWNT branches when AC voltage (16V peak-to-peak at 1 MHz ) is applied for (a) a pair of parallel electrodes; (b) cross electrodes; (c) T-electrodes.

Fig. 2.  Complex polarization factor K when the longest axis of the MWNT is parallel to the electric field applied.

Fig. 11. Plots of statistical data of measured resistances between the Au microelectrodes on different samples.

Fig. 15. Schematic diagram showing the constant current mode circuit configuration.

Fig. 12. TCR variations of a typical MWNT device in five consecutive measurements.  The experimental data are linearized for the approximation of TCRs.

Fig. 14. I-V characteristics of the MWNT bundles. Three repeated measurements were performed to validate the repeatability. The straight line is the theoretical expectation using Ohm’s Law and the room temperature resistance of bundled MWNTs in our testing sample was about 170kΩ.

Fig. 16. Frequency response of the constant current circuit with bundled MWNT as feedback resistor. The cutoff frequency was estimated to be 177kHz according to [36].

Fig. 9. (a) Photograph of the fabricated array of Au microelectrodes on a substrate. (b) Optical image showing a pair of Au microelectrodes before CNT manipulation.

Fig. 7. Optical microscopic images (A-F) showing the process of AC electrophoretic manipulation of bulk MWNTs. Consecutive pictures were captured with 6 seconds intervals. (Scale bar = 20 µm)

Fig. 10. (a) Drawing of the design for the chip with arrays of Au microelectodes. (b) Scanning electron microscopic (SEM) images showing the formations of MWNTs between different pairs of Au microelectrodes.

Fig. 1. A dielectric spherical particle is undergoing dielectrophoretic motion. The unbalanced force impart on the sphere causing it to move towards the smaller electrode.  The figure above showing the charge distribution in a particular instant where the small electrode is at a higher potential than the large electrode.  For AC bias voltage, the potential will be interchanged periodically on the electrodes and the resulting force on the particle is still acting on the same direction due to uneven electric field distribution.

Fig. 4. Average DEP force between the electrodes which were applied by  16V peak-to-peak AC voltage at 1MHz. Arrows are the force vectors on x-y plane (a) at 1 µm and (b) 3 µm, respectively, above the electrodes in Fig. 3a. The contours represent the order of downward forces.

Fig. 5. Average DEP force between the electrodes when AC voltage (16V peak-to-peak at 1MHz) is applied for  (a) cross electrodes and (b) T-electrodes at 3 µm above the surface.

Fig. 13. Room temperature resistance drifting of the CNT sensors during seven repeated thermal cycling.